AQUAPANEL® Cement Board Floor

Dry floor with reinforced load-distributing layer load

capacity up to 4.0 kN/ m2 (Variant 1)

Specification examples

| Item | Quantity / ME | Description of service | Unit cost | Total cost |
| --- | --- | --- | --- | --- |
|  | m2 m2 m2 m2 m2 m2 m2 | Prepare, clean solid floor for receiving a dry floor. In the case of floors without basements: Apply a moisture barrier in acc. with DIN 18195 made of ___________________________, which is guided approx. _________ cm high (up to further horizontal sealing in the walls). In the case of new concrete floors or above wet rooms: Lay polyethylene film (e.g. 0.2 mm) loosely with 50 cm overlap. AQUAPANEL® Levelling Fill, installation thickness (d<60mm) ________ mm, must be removed with a superelevation of 10% flat with the plane over gauges. Uneven areas, pipes or cables must be covered by at least 10 mm. Lay cover panels (e.g. soft timber fibres, mineral fibres, plasterboard in accordance with EN520; note material thickness for layer height), tight against one another, avoiding cross joints and shifted to the joints on the fill. Lay AQUAPANEL® Cement Board Indoor (12.5 mm cement-bonded building panel) tight against one another, avoiding cross joints and shifted to the joints on the cover panel accordance with the processing instructions of Knauf Aquapanel GmbH & Co. KG. Lay AQUAPANEL® Cement Board Floor, 22 mm, cement-bonded dry floor element with surrounding slot, transverse to the laying direction of the AQUAPANEL® Cement Board Floor. Adhesion is carried out by AQUAPANEL® Joint Adhesive (PU) or AQUAPANEL® Slot Adhesive (PU) which is applied in beads with a spacing of approx. 10 cm. |  |  |